## Slide 1: Maurits W. Haverkort
Theoretical Physics
Institute for
Calculating photoemission, x-ray absorption, RIXS, and …
with Quanty

## Slide 2: X-rays for the study of Quantum materials
Many non-trivial emergent phenomena in Quantum materials
For example high Tc superconductivity

## Slide 3: X-rays for the study of Quantum materials
Or metal insulator phase transitions
M. Marezio et al.,
PRB 5, 2541 (1972)
P. B. Allen et al.,
PRB 48, 4359 (1993)
Many non-trivial emergent phenomena in Quantum materials

## Slide 4: Example metal insulator transition in VO2
M. Marezio et al.,
PRB 5, 2541 (1972)
P. B. Allen et al.,
PRB 48, 4359 (1993)
Phase transitions in simple materials
Low temperature: Insulator without excitations
Intermediate temperature: Insulator with excitations
High temperature: Metal

## Slide 5: Example metal insulator transition in VO2
M. Marezio et al.,
PRB 5, 2541 (1972)
P. B. Allen et al.,
PRB 48, 4359 (1993)
Optical gap in VO2
H.W. Verleur et al.,
Phys. Rev. 172, 788 (1968)

## Slide 6: Example metal insulator transition in VO2
M. Marezio et al.,
PRB 5, 2541 (1972)
P. B. Allen et al.,
PRB 48, 4359 (1993)
Optical gap in VO2
H.W. Verleur et al.,
Phys. Rev. 172, 788 (1968)
Collective phenomena

## Slide 7: Interactions between lattice, charge, orbital and spin
lattice
orbital
charge
spin

## Slide 8: Challenges in describing correlated Quantum materials
Coulomb energy
Potential energy and Darwin term
Spin orbit interaction
Kinetic energy with mass correction term
For fixed nuclear positions that define the potential

## Slide 9: Challenges in describing correlated Quantum materials
Potential energy and Darwin term
Spin orbit interaction
Kinetic energy with mass correction term
For fixed nuclear positions that define the potential
(Mean-field) Coulomb potential

## Slide 10: Mean-field calculations – matrix formalism
Define a basis of spin-orbitals
es
ep
ep
ep
Hamiltonian is represented by a matrix on this basis

## Slide 11
Quantum mechanics in matrix formalism – multi electron
Define a basis of many electron wave-functions (states)
es
Hamiltonian is a matrix on this basis
ep
ep
ep
es+ep+Usp
es+ep+Usp
es+ep+Usp
2ep+Upp
2ep+Upp
2ep+Upp
es+2ep
+2Usp+Upp
es+2ep
+2Usp+Upp
3ep
+3Upp
es+2ep
+2Usp+Upp
0
…
_

## Slide 12
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2
1
Cluster of H atom
only include the 1s orbital

## Slide 13
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
2
1
4
2
Cluster of H atom
only include the 1s orbital

## Slide 14
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
2
1
4
2
8
4
Cluster of H atom
only include the 1s orbital

## Slide 15
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
6 | 12 | 6 |  | ( ) | 924
2
1
4
2
8
4
12
6
Cluster of H atom
only include the 1s orbital

## Slide 16
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
6 | 12 | 6 |  | ( ) | 924
8 | 16 | 8 |  | ( ) | 12 870
2
1
4
2
8
4
12
6
16
8
Cluster of H atom
only include the 1s orbital

## Slide 17
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
6 | 12 | 6 |  | ( ) | 924
8 | 16 | 8 |  | ( ) | 12 870
10 | 20 | 10 |  | ( ) | 184 756
2
1
4
2
8
4
12
6
16
8
20
10
Cluster of H atom
only include the 1s orbital

## Slide 18
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
6 | 12 | 6 |  | ( ) | 924
8 | 16 | 8 |  | ( ) | 12 870
10 | 20 | 10 |  | ( ) | 184 756
12 | 24 | 12 |  | ( ) | 2 704 156
2
1
4
2
8
4
12
6
16
8
20
10
24
12
Cluster of H atom
only include the 1s orbital

## Slide 19
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
6 | 12 | 6 |  | ( ) | 924
8 | 16 | 8 |  | ( ) | 12 870
10 | 20 | 10 |  | ( ) | 184 756
12 | 24 | 12 |  | ( ) | 2 704 156
14 | 28 | 14 |  | ( ) | 40 116 600
2
1
4
2
8
4
12
6
16
8
20
10
24
12
28
14
Cluster of H atom
only include the 1s orbital

## Slide 20
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
6 | 12 | 6 |  | ( ) | 924
8 | 16 | 8 |  | ( ) | 12 870
10 | 20 | 10 |  | ( ) | 184 756
12 | 24 | 12 |  | ( ) | 2 704 156
14 | 28 | 14 |  | ( ) | 40 116 600
16 | 32 | 16 |  | ( ) | 601 080 390
2
1
4
2
8
4
12
6
16
8
20
10
24
12
28
14
32
16
Cluster of H atom
only include the 1s orbital

## Slide 21
Exponential scaling of quantum mechanics
Example cluster of H atoms
# atoms
# spin-
orbitals
# electrons
# states
1 | 2 | 1 |  | ( ) | 2
2 | 4 | 2 |  | ( ) | 6
4 | 8 | 4 |  | ( ) | 70
6 | 12 | 6 |  | ( ) | 924
8 | 16 | 8 |  | ( ) | 12 870
10 | 20 | 10 |  | ( ) | 184 756
12 | 24 | 12 |  | ( ) | 2 704 156
14 | 28 | 14 |  | ( ) | 40 116 600
16 | 32 | 16 |  | ( ) | 601 080 390
18 | 36 | 18 |  | ( ) | 9 075 135 300
2
1
4
2
8
4
12
6
16
8
20
10
24
12
28
14
32
16
36
18
Cluster of H atom
only include the 1s orbital

## Slide 22
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
16
14
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)
Exponential scaling of quantum mechanics

## Slide 23
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
2 | 32 | 28 |  | ( ) | 35 960
16
14
32
28
Exponential scaling of quantum mechanics
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)

## Slide 24
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
2 | 32 | 28 |  | ( ) | 35 960
3 | 48 | 42 |  | ( ) | 12 271 512
16
14
32
28
48
42
Exponential scaling of quantum mechanics
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)

## Slide 25
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
2 | 32 | 28 |  | ( ) | 35 960
3 | 48 | 42 |  | ( ) | 12 271 512
4 | 64 | 56 |  | ( ) | 4 426 165 368
16
14
32
28
48
42
64
56
Exponential scaling of quantum mechanics
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)

## Slide 26
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
2 | 32 | 28 |  | ( ) | 35 960
3 | 48 | 42 |  | ( ) | 12 271 512
4 | 64 | 56 |  | ( ) | 4 426 165 368
5 | 80 | 70 |  | ( ) | 1 646 492 110 120
16
14
32
28
48
42
64
56
80
70
Exponential scaling of quantum mechanics
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)

## Slide 27
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
2 | 32 | 28 |  | ( ) | 35 960
3 | 48 | 42 |  | ( ) | 12 271 512
4 | 64 | 56 |  | ( ) | 4 426 165 368
5 | 80 | 70 |  | ( ) | 1 646 492 110 120
6 | 96 | 84 |  | ( ) | 624 668 654 531 480
16
14
32
28
48
42
64
56
80
70
96
84
Exponential scaling of quantum mechanics
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)

## Slide 28
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
2 | 32 | 28 |  | ( ) | 35 960
3 | 48 | 42 |  | ( ) | 12 271 512
4 | 64 | 56 |  | ( ) | 4 426 165 368
5 | 80 | 70 |  | ( ) | 1 646 492 110 120
6 | 96 | 84 |  | ( ) | 624 668 654 531 480
7 | 112 | 98 |  | ( ) | 240 260 199 935 164 200
16
14
32
28
48
42
64
56
80
70
96
84
112
98
Exponential scaling of quantum mechanics
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)

## Slide 29
Example NiO
# unit cells
# spin-
orbitals
# electrons
# states
1 | 16 | 14 |  | ( ) | 120
2 | 32 | 28 |  | ( ) | 35 960
3 | 48 | 42 |  | ( ) | 12 271 512
4 | 64 | 56 |  | ( ) | 4 426 165 368
5 | 80 | 70 |  | ( ) | 1 646 492 110 120
6 | 96 | 84 |  | ( ) | 624 668 654 531 480
7 | 112 | 98 |  | ( ) | 240 260 199 935 164 200
… |  |  |  |  | 
16
14
32
28
48
42
64
56
80
70
96
84
112
98
Exponential scaling of quantum mechanics
NiO
Ni 3d and O 2p per unit cell
On LDA level NiO is metallic (in reality a good insulator)

## Slide 30: Many advanced methods available
Some work for some properties of some materials, none work for all
Hartree-Fock approximation
Density functional theory
Configuration interaction
Coupled Cluster
Restrictive Active Space
Renormalization group theory
Tensor network states
Cluster expansion
Dynamical mean-field theory
DΓA
Quantum Montecarlo

## Slide 31: Need advanced tools to measure
Spin arrangements (element resolved of TM multilayers)
Valence and local symmetry of TM compounds
Orbital occupation (the d (f)-shell is 5 (7) fold degenerate)
dyz
dxz
dxy
dx2-y2
d3z2-r2
And excitations (spin-waves – magnons – orbital excitations)
How the low energy Hamiltonian emerges from the full Hamiltonian
Use spectroscopies

## Slide 32
Spectroscopy as a tool to test and learn
PES
Optics

## Slide 33
X-ray spectroscopy as a tool to test and learn
PES
XAS
RXD
RIXS
nIXS

## Slide 34: Example XAS on VO2
M. Marezio et al.,
PRB 5, 2541 (1972)
P. B. Allen et al.,
PRB 48, 4359 (1993)
PRL 95, 196404 (2005)
Need theory to extract information from the spectra

## Slide 35: Need theory to relate the material properties to the spectra
Merged in a script language
Not structure in result out.
You need to do some programming / modeling
Different models
Levels of theory
Crystal-field
Ligand-field
Anderson Impurity (DMFT)
DFT
Spin-wave theory
…
Different spectroscopies
PES ESR
IPES NMR
cPES STM
Optics Magnetization
XAS Specific heat
RXD …
RIXS
nIXS
XES Please list your
FY publications at
EC www.quanty.org

## Slide 36: Quanty script for a crystal field calculation on Ni in NiO

## Slide 37: Some theoretical background
Second quantization
Response theory
Green’s functions
Model optimization
See also lecture notes on Youtube
https://www.youtube.com/@MauritsHaverkort

## Slide 38: Some theoretical background
Second quantization
Response theory
Green’s functions
Model optimization
See also lecture notes on Youtube
https://www.youtube.com/@MauritsHaverkort

## Slide 39
Introducing language – Second quantization
with
Many particle wave function
Youtube

## Slide 40
Many particle wave function
Introducing language – Second quantization
For H atom
  One particle orbital
  With quantum number
Youtube

## Slide 41
Many particle wave function
Introducing language – Second quantization
For He atom
  One particle orbital
  With quantum number
Assume orbitals have similar structure as H orbitals and take as an ansatz the state:
with
And optimize to find lowest energy
Youtube

## Slide 42
Many particle wave function
Introducing language – Second quantization
One problem: 4 solutions
  One particle orbital
  With quantum number
They are all orthogonal to each other
  Pauli: postulate: no math reason, but new physics:
Two electrons can not be in the same spin-orbital
Youtube

## Slide 43
Many particle wave function
Introducing language – Second quantization
One problem: 4 solutions
  One particle orbital
  With quantum number
They are all orthogonal to each other
  Pauli: postulate: no math reason, but new physics:
Two electrons can not be in the same spin-orbital
  Oh Oh still two states left …. Eh ….
  Must hold for any basis, see what happens when rotating the spin quantization axis
Youtube

## Slide 44
Introducing language – Second quantization
Youtube

## Slide 45
Introducing language – Second quantization
Youtube

## Slide 46
Many particle wave function
Introducing language – Second quantization
He ansatz wavefunction
  One particle orbital
  With quantum number
Two electrons can not be in the same spin-orbital for any basis (anti-symmetrize)
  Pauli: postulate: no math reason, but new physics:
Youtube

## Slide 47
Many particle wave function
Introducing language – Second quantization
He ansatz wavefunction
  One particle orbital
  With quantum number
Two electrons can not be in the same spin-orbital for any basis (anti-symmetrize)
  Pauli: postulate: no math reason, but new physics:
Youtube

## Slide 48
  Single Slater determinant
Many particle wave function
Introducing language – Second quantization
He ansatz wavefunction
  One particle orbital
  With quantum number
Youtube

## Slide 49
Introducing language – Second quantization
Li ansatz wavefunction
Youtube

## Slide 50
Introducing language – Second quantization
Ne ansatz wave function
  Not practical, need a different notation
Youtube

## Slide 51
Introducing language – Second quantization
Youtube

## Slide 52
Introducing language – Second quantization
Youtube

## Slide 53
Introducing language – Second quantization
Youtube

## Slide 54
Introducing language – Second quantization
Paul: postulate: no math reason, but new physics:
Two electrons can not be in the same spin-orbital for any basis (anti-symmetrize)
Youtube

## Slide 55
Introducing language – Second quantization
  One particle orbital
  With quantum number
  Single Slater determinant
Many particle wave function
Youtube

## Slide 56
Operators in second quantization
How to calculate:
or:
Distinguish two cases

## Slide 57
Operators in second quantization
One particle operators
Two particle operators

## Slide 58
Operators in second quantization
with,
with,
Proof: homework
One particle operators
Two particle operators

## Slide 59: Some theoretical background
Second quantization
Response theory
Green’s functions
Model optimization
See also lecture notes on Youtube
https://www.youtube.com/@MauritsHaverkort

## Slide 60: Response theory – photon absorption
Due to the external electromagnetic field the electron moves in space
A change in position yields the induced dipole moment (p)
The velocity of the electron proportional to the induced current (j)
The change in current over time yields the acceleration of the electrons
Youtube
Absorption is movement against a force
Accelerated electrons radiate photons - diffraction

## Slide 61: Measurements: Response theory
How does the system react when you act on it
Volterra series expansion
Youtube
Energy conservation
It does not matter if we do our experiment today or tomorrow
Fourier transform

## Slide 62: Measurements: Response theory
Youtube
How does the system react when you act on it
Volterra series expansion
Fourier transform

## Slide 63: Measurements: Response theory
Youtube
How does the system react when you act on it
Volterra series expansion
Relation between susceptibility and experimental observables
Polarizability
Absorption
Diffraction

## Slide 64: How to calculate the susceptibility – Kubo
Youtube
System given by Hamiltonian H and time dependent perturbation H1
With Fourier transforms
Measure operator O

## Slide 65: Relation to Fermis golden rule
Youtube

## Slide 66
Example on an H2 molecule
1s
1s

## Slide 67
Example on an H2 molecule
1s
1s

## Slide 68
Example on an H2 molecule
1s
1s

## Slide 69
Example on an H2 molecule
Excitation energy
Intensity

## Slide 70
Example on an H2 molecule – with correlations

## Slide 71
Example on an H2 molecule – with correlations

## Slide 72
Example on an H2 molecule – with correlations

## Slide 73
Example on an H2 molecule – with correlations
Excitation energy
Intensity

## Slide 74
Example on an H2 molecule – with correlations
Excitation energy
Intensity
1s
1s

## Slide 75: Challenges in calculation
Calculate the many-body ground-state
Calculate the effect of the operator O on the ground-state
Calculate the time evolution of state

## Slide 76: The transition operator – photon matter interactions
Calculate the effect of the operator O on the ground-state
Photons, neutrons, electrons, … only interact with one electron simultaneously.

## Slide 77: The transition operator – photon matter interactions
Calculate the effect of the operator O on the ground-state
Photons, neutrons, electrons, … only interact with one electron simultaneously.
Youtube

## Slide 78: Challenges in calculation
Calculate the many-body ground-state
Calculate the effect of the operator O on the ground-state
Calculate the time evolution of state

## Slide 79
Three classes of excitations
Band excitations
Resonances
Excitons

## Slide 80
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
Core – valence interaction
W=1
U=20
Q=0

## Slide 81
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=0.25

## Slide 82
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=0.5

## Slide 83
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.0

## Slide 84
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.25

## Slide 85
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.5

## Slide 86
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.75

## Slide 87
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=2.0
Exciton
Continuum edge jump

## Slide 88
Three classes of excitations
Band excitations
Resonances
Excitons

## Slide 89
X-ray absorption spectroscopy – a band picture
1s

## Slide 90
Three classes of excitations
Band excitations
Resonances
Excitons

## Slide 91
X-ray absorption spectroscopy – excitons
2p

## Slide 92
X-ray absorption spectroscopy – excitons
2p

## Slide 93
Local many body calculations based on parameters

## Slide 94
Local many body calculations based on parameters
Parameters
Size of the Coulomb interaction
Size of the crystal-field

## Slide 95
How to calculate these parameters
2p
Start from LDA potential
Create Wannier functions
On this basis and potential build local Hamiltonian including all local many body interactions
Solve by exact diagonalization
Phys. Rev. B 85, 165113 (2012)
Theory
Experiment
M.W. Haverkort, M. Zwierzycki, O.K. Andersen, PRB 85, 165113 (2012).

## Slide 96
What do you need to consider when calculating excitons
Example of d-d excitations in NiO

## Slide 97
Example of localized states in NiO - excitons
Ni2+ - 4s0 3d8
O2- - 2p6

## Slide 98
Partly filled degenerate d-shell – in LDA NiO is a metal

## Slide 99
In LDA NiO is a metal: Experimentally it is a good insulator
F. J. Morin, Phys. Rev. 93, 1199 (1954)
R. Newman and R. M. Chrenko,
Phys. Rev 114 1507 (1959)
Room temperature
r~105 W cm
Optical-gap
3.5 – 4.0 eV
Conductivity (W-1 cm-1)
Temperature-1
Local d-d excitations inside the optical gap. Week in optics as NiO has inversion symmetry, i.e. they are dipole forbidden

## Slide 100
d-d excitations inside gap (inelastic x-ray scattering)
Theory M. W. Haverkort et al. PRL 99, 257401 (2007)
Beyond – dipole
1 eV loss of
10 000 eV photons

## Slide 101
Orbital energy level diagram
t2g
eg

## Slide 102
First peak, excitation from t2g to eg
M. W. Haverkort et al. PRB 85, 165113 (2012)
First peak, understandable on the level of LDA+U

## Slide 103
Third peak – Coulomb repulsion
dxy
dx2-y2
dz2
Coulomb repulsion is smaller when electrons are farther apart

## Slide 104
Third peak – Coulomb repulsion
dx2-y2
dz2
dxy
dxy
Coulomb repulsion is smaller when electrons are farther apart

## Slide 105
Third peak – Coulomb repulsion
M. W. Haverkort et al. PRB 85, 165113 (2012)
Third peak understandable on the level of time dependent LDA+U

## Slide 106
Second peak, double excitation from t2g to eg
M. W. Haverkort et al. PRB 85, 165113 (2012)
DMFT with ED solver
Mix of DMRG and Quantum Chemistry

## Slide 107
Second peak, double excitation from t2g to eg
M. W. Haverkort et al. PRB 85, 165113 (2012)
Warning!!! A single photon can only excite a single electron. The reason you see these strong double excitations is a true quantum many-body effect!
- Need to solve locally the full many-body problem

## Slide 108
Three classes of excitations
Band excitations
Resonances
Excitons

## Slide 109
Interaction between localized and delocalized states
Elastic line
Local excitons
(d-d excitations)
Itinerant excitations
(charge-transfer)
M. W. Haverkort et al. EPL 108, 57004 (2014)

## Slide 110
Interaction between localized and delocalized states
Elastic line
Local excitons
(d-d excitations)
Itinerant excitations
(charge-transfer)
M. W. Haverkort et al. EPL 108, 57004 (2014)

## Slide 111
Interaction between localized and delocalized states (MnO)
LDA+Ligand – Field
LDA+DMFT

## Slide 112
Multipole expansion – |q| dependence
J. A. Bradley et al.,
Phys. Rev. B 84, 205105 (2011).
R. A. Gordon, et al.
Euro. Phys. Lett. 81, 26004 (2008)
Phys. Rev. Lett. 99, 257401 (2007)
Why are the multipole excitations at lower energy so much sharper and thus clearer to see?

## Slide 113: Some theoretical background
Second quantization
Response theory
Green’s functions
Model optimization
See also lecture notes on Youtube
https://www.youtube.com/@MauritsHaverkort

## Slide 114: NiO – Density functional theory

## Slide 115: NiO – Crystal field theory
Approximate a solid by a single atom + external effective potential

## Slide 116: NiO – Crystal field theory
Approximate a solid by a single atom + external effective potential

## Slide 117: NiO – Crystal field theory
Approximate a solid by a single atom + external effective potential

## Slide 118: NiO – Ligand field theory
Approximate a solid by a single atom +
ligand atoms (linear combinations of O atoms)

## Slide 119: NiO – Ligand field theory
Approximate a solid by a single atom +
ligand atoms (linear combinations of O atoms)

## Slide 120: NiO – Ligand field theory
Approximate a solid by a single atom +
ligand atoms (linear combinations of O atoms)

## Slide 121: NiO – Ligand field theory
Approximate a solid by a single atom +
ligand atoms (linear combinations of O atoms)

## Slide 122: NiO – Ligand field theory
Approximate a solid by a single atom +
ligand atoms (linear combinations of O atoms)

## Slide 123: NiO – Ligand field theory
Approximate a solid by a single atom +
ligand atoms (linear combinations of O atoms)

## Slide 124: Obtain a crystal-field from a ligand field Hamiltonian
Orbital dependent “dilution” of Coulomb interaction

## Slide 125: Anderson impurity model
Different geometries to represent the bath

## Slide 126: Anderson impurity model
Use Schur’s formula for matrix inversion
A
B
Youtube

## Slide 127: Example – Auger-Meitner lifetime of core holes
Atomic Hamiltonian only including bound states
Coulomb operator
Atomic Hamiltonian with one free electron

## Slide 128: Auger-Meitner lifetime in Ho – Dy nuclear transition

## Slide 129: Example – Fluorescence lifetime of core holes
Atomic Hamiltonian without photons
Electron photon interaction
Atomic Hamiltonian with one photon

## Slide 130: Fluorescence lifetime in Mn – Fe nuclear transition

## Slide 131: Fluorescence lifetime in Mn – Fe nuclear transition

## Slide 132: Fluorescence lifetime in Mn – Fe nuclear transition

## Slide 133: Mixing of states with different photon number

## Slide 134: Resonances in RIXS – Ce f-f transitions

## Slide 135: Dynamical mean-field theory
What are the parameters of the Bath in an Anderson impurity model
Youtube

## Slide 136: DMFT – short introduction
Two atoms interacting with each other
A
B
Define a non-interacting reference system such that it has the same Green’s function as G(BB,ω)
Youtube

## Slide 137: DMFT – short introduction

## Slide 138: Some theoretical background

## Slide 139
XAS and the conductivity tensor (s) – an example for s to p
w0
Real
Imaginary
Absorption –Im[s]
(in Landau Lifschitz absorption is Re[s])

## Slide 140
But the conductivity tensor (s) is a TENSOR

## Slide 141
But the conductivity tensor (s) is a TENSOR
Absorption
–Im[e.s.e]

## Slide 142
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
x-polarized light

## Slide 143
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
y-polarized light

## Slide 144
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
z-polarized light

## Slide 145
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
Absorption
–Im[e.s.e]

## Slide 146
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light

## Slide 147
The conductivity tensor (s) in cubic symmetry

## Slide 148
The conductivity tensor (s) in tetragonal symmetry

## Slide 149
The conductivity tensor (s) in orthorhombic symmetry

## Slide 150
The conductivity tensor (s) in monoclinic symmetry

## Slide 151
The conductivity tensor (s) in triclinic symmetry

## Slide 152
The conductivity tensor (s) in magnetic materials

## Slide 153
The conductivity tensor (s) in magnetic materials

## Slide 154
Sum rules for circular dichroism: orbital and spin momentum

## Slide 155
Thole et al.’s sum-rules in tensor form. s to p excitations

## Slide 156
Resonant X-ray Diffraction (RXD)
2p
And now momentum, i.e. spatial resolved, from XAS to RXD
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Hannon, Trammel, Bloom, Gibbs
Phys. Rev. Lett. 61, 1245 (1988)
Phys. Rev. B 43, 5663 (1991)
Cara, Thole
Rev. Mod. Phys. 66, 1509 (1994)

## Slide 157
An example magnetic Bragg reflection of Ho metal film
2p

## Slide 158
An example magnetic Bragg reflection of Ho metal film

## Slide 159
Absorption and diffraction – two sides of the same coin
Polarizability: displacement of the electron
Conductivity: movement of the electron
Scattering length: acceleration of the electron

## Slide 160
Crystalline solid
Absorption and diffraction – two sides of the same coin
si
si
si
si
Each site gets polarized by the photon field and the local charge density starts to oscillate.
Absorption
Scattering

## Slide 161
2p
Relation between resonant x-ray diffraction and absorption
2p

## Slide 162
Diffraction at given momentum determined by the sum of local scattering with correct phase:
Crystalline sollid
Absorption and diffraction – two sides of the same coin
si
si
si
si
Each site gets polarized by the photon field and the local charge density starts to oscillate.
Absorption
Scattering

## Slide 163
An example magnetic Bragg reflection of Ho metal film

## Slide 164
Fundamental spectra from the literature

## Slide 165
Fundamental spectra from the literature

## Slide 166
Fundamental spectra from the literature

## Slide 167
Fundamental spectra from the literature

## Slide 168
An example magnetic Bragg reflection of Ho metal film

## Slide 169
Can we use sum-rules to get quantitative information

## Slide 170
Can we use sum-rules to get quantitative information

## Slide 171
Can we use sum-rules to get quantitative information

## Slide 172
Can we use sum-rules to get quantitative information

## Slide 173
Can we use sum-rules to get quantitative information

## Slide 174
Can we use sum-rules to get quantitative information

## Slide 175
Solve Maxwell's equations (with side conditions)

## Slide 176
2p
2p
And now excitations , from RXD to RIXS
2p
X-ray Absorption
Spectroscopy
Resonant X-ray
Diffraction
Resonant Inelastic
X-ray scattering

## Slide 177
Dispersing magnons

## Slide 178
Dispersing magnons – Neutron scattering
Interaction of Neutrons with matter is well understood (magnetic dipole),
single magnon intensity
q-dispersion
M. T. Hutchings and E. J. Samuelsen,
Phys. Rev. B 6, 3447 (1972)

## Slide 179
Recent development – measure spin dynamics with x-rays
Picture by G. Ghiringhelli and L. Braicovich
Resonant Inelastic
X-ray Scattering
RIXS
It now becomes feasible to measure the dynamics of low energy excitations in:
thin films
surfaces
Interfaces
nano-crystals
molecules

## Slide 180
RIXS – very high quality data on small samples
L. Braicovich, et al. LaSrCuO4, PRL 104, 077002 (2010)

## Slide 181
RIXS – very high quality data on small samples
spinons
orbitons
Schlappa, et al. Sr2CuO3, Nature 485 82 (2012)

## Slide 182
What is Resonant Inelastic X-ray Scattering (RIXS)
Outgoing light of
~ 0.5 to 10 keV
minus
10 meV to 10 eV
Incoming light of
~ 0.5 to 10 keV
Intermediate state with core hole and one extra valence electron

## Slide 183
Intermediate state
RIXS – what does one measure
Initial state
Final state

## Slide 184
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 185
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 186
RIXS – what is the cross section
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…

## Slide 187
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 188
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 189
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 190
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 191
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 192
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 193
XAS – XRD – RIXS – a time dependent picture

## Slide 194
XAS – XRD – RIXS – a time dependent picture in NiO
eg
t2g

## Slide 195
NiO – Ni 2p to Ni 3d excitation
eg
t2g
Ni-3d and O-2p on level of DMFT. (locally all interactions included)
Ni-3d and Ni-2p Coulomb interactions are local and included
After excitation Auger decay is possible, and included:
Ni-3d, Ni-3p, or Ni-3s scatters into the Ni-2p core hole and a Ni-3d, Ni-3p or Ni-3s orbital is emitted into es,p,d,f,g or h orbital

## Slide 196
NiO – Ni 2p to Ni 3d excitation
X-ray absorption of NiO (L23 edge) is well described.
How does the wave-function (charge density) evolve as a function of time when the sample is hit by an x-ray pulse?

## Slide 197
NiO – Ni 2p to Ni 3d excitation
eg
t2g
We include a light field of 1 kV per Angstrom (possible at SLAC) at an energy of 852 eV.
Pulse duration is 100 atto seconds
Upto c7 (4-th-order) response functions are included

## Slide 198
NiO 2p to 3d excitation in the time domain
1 kV Å-1
350 attosecond
holes in Ni 3d-shell
holes in Ni 2p-shell
FWHM 100 as
41 eV
Energy of pulse 852 eV

## Slide 199
Magnetic excitations in NiO
Abhishek Nag, …, Ke-Jin Zhou, NiO, PRL 124, 067202 (2020)

## Slide 200
Single and double magnon excitations in NiO
Abhishek Nag, …, Ke-Jin Zhou, NiO, PRL 124, 067202 (2020)

## Slide 201
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 202
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
BOOM
RIXS – what does one measure

## Slide 203
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 204
Challenge – No small parameter – perturbation theory fails
Different interactions are of similar scale
Perturbation theory leads to divergent series
i.e. summing part of the series gives a different result from the full solution!

## Slide 205
Intermediate state
Initial state
Final state
RIXS – what does one measure

## Slide 206
Relations between absorption, elastic- and inelastic scattering
The elastic scattering tensor is related to the absorption by the optical theorem (Conservation of energy)
Elastic scattering is a limiting case of inelastic scattering:
If one restricts the inelastic scattering operator R to the ground-state one describes the elastic scattering
For the description of magnetic excitations:
Expand the scattering operator on spin operators
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 207
Understand RIXS by numerical solving a model
The equation to solve
with,
and

## Slide 208
Single Ni atom in crystal-field theory

## Slide 209
Hubbard model on finite (12) size cluster

## Slide 210
Understand RIXS as effective operator
Replace the exact RIXS operator by a low energy effective operator
Write the exact RIXS operator as a series
Possible operators in the series could be
Task: find all operators
and all coefficients

## Slide 211
Challenge – No small parameter – perturbation theory fails
Different interactions are of similar scale
Perturbation theory leads to divergent series
i.e. summing part of the series gives a different result from the full solution!

## Slide 212
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 213
Truncate at i=2
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 214
Truncate at i=4
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 215
Truncate at i=10
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 216
Truncate at i=20
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 217
Truncate at i=50
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 218
General problem in many particle physics

## Slide 219
General problem in many particle physics
Need for a non-divergent (non perturbative) series expansion

## Slide 220
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:

## Slide 221
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=1

## Slide 222
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=2

## Slide 223
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=3

## Slide 224
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=4

## Slide 225
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=5

## Slide 226
An alternative expansion for operators
Projection expansions for functions
Projection expansions for operators
with
if
with
if

## Slide 227
An alternative expansion for operators
Trivial example
with
and
an orthonormal complete set
we have
The trivial example needs exponentially many weird operators
Alternative:
Om,n an operator that transforms exponentially many states that share property n into states that share property m

## Slide 228
Expansion of the RIXS operator
Create a local (j) expansion
Lattice model

## Slide 229
Expansion of the RIXS operator
Lattice model
Site j
Create a local (j) expansion
Level L=0 only include operators acting on site j

## Slide 230
Expansion of the RIXS operator
Lattice model
Create a local (j) expansion
Level L=1 include operators acting on site j and n.n.
j

## Slide 231
Expansion of the RIXS operator
Lattice model
Create a local (j) expansion
Level L=2 include operators acting on site j, n.n. and n.n.n.
j

## Slide 232
Expansion of the RIXS operator
Lattice model
Create a local (j) expansion
Level L=3 include operators acting on site j, n.n., n.n.n. and n.n.n.n.
j
etc.

## Slide 233
Expansion of the RIXS operator
Convergence of this series is guaranteed by linear algebra!
define

## Slide 234
Expansion of the RIXS operator
Convergence of this series is guaranteed by linear algebra!
As RIXS intensity is bounded:
Sufficient condition to guarantee absolute convergence of series

## Slide 235
Example for doped Hubbard model
with
As a first step we need to create all possible Om,n
For L=0 we only look at local operators
The local Fock space is given by 4 states
Operators on that basis as
4 by 4 matrices

## Slide 236
For L=1 we look at two sites
Example for doped Hubbard model
Resulting in 162=256 operators
The Fock space is given by 16 states

## Slide 237
We can get back to more familiar representations by linear combing these operators (unitary transformation)
Example for doped Hubbard model
For L=0 (only keeping the particle number conserving operators)

## Slide 238
We can get back to more familiar representations by linear combing these operators (unitary transformation)
Example for doped Hubbard model
For L=1 (only keeping the particle number conserving operators)

## Slide 239
RIXS – effective operator – spin excitations
Effective operator for spin excitations only

## Slide 240
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
… and spin susceptibilities

## Slide 241
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
Theory
Experiment
s(0)=

## Slide 242
Predicted RIXS spectra with cross polarized light
spin susceptibility, same as neutron scattering

## Slide 243
General polarization: RIXS is a mixture of 1 and 2 spin flips

## Slide 244
Spin excitations in 1-dimension

## Slide 245
Spin excitations in 1-dimension
S. Glawion, …, R. Claessen, TiOCl, PRL 107, 107402 (2011)

## Slide 246
Spin excitations in 1 dimension – Sr2CuO3

## Slide 247
Dispersing orbitals
spinons
orbitons

## Slide 248
Dispersing orbitals

## Slide 249
Dispersing orbitals

## Slide 250
Additional information
Code to calculate core level spectroscopy
www.quanty.org
YouTube lectures on solid state physics
https://www.youtube.com/c/MauritsHaverkort

## Slide 251
Graphical interface to Quanty