## Slide 1: Core level spectroscopy of transition metal and rare earth compounds
Transition metal and rare earth compounds show a wealth of different properties. They are used as materials for energy storage (battery compounds), dyes in solar cells, elements in the read head of hard disks, high temperature superconductors, or the active centers in many of the known enzymes. The large variety of tunable properties of these materials is related to the large number of low energy degrees of freedom of the transition metal or rare earth ion. Correlations between the electrons in a solid lead to a detailed interplay between the local spin, charge, orbital and lattice degrees of freedom. The result is extremely rich physics of these open shell systems. At the same time the interplay between several low energy degrees of freedom make these materials involved to understand. Although enormous theoretical progress has been made during the last years in the understanding of correlated materials one often needs experimental input to understand particular phenomenon.
Core level spectroscopy in many cases turns out to be a very efficient method to study the many body properties of these systems. Core level photoelectron spectroscopy allows one to determine how the low energy Hamiltonian arises from the high-energy scale interactions. It thus provides information on the low energy model parameters of the system. X-ray absorption spectroscopy contains information on the local electronic structure. It provides information on the symmetry of the wave function, such as the local spin-state or orbital occupation. Resonant x-ray diffraction is related to x-ray absorption, in addition to x-ray absorption it allows one to study the special dependence of local electronic order in the system. Resonant inelastic x-ray scattering allows one to study the dynamics of low energy excitations. Non-resonant inelastic x-ray scattering of core level excitations is a technique rather comparable to x-ray absorption spectroscopy with the difference that it allows for non-dipole transitions, useful in the study of involved orbital or multipole ordering.
For the understanding of these spectra, in this class of materials, it is important to realize that one needs to treat the interactions between the electrons beyond mean field approximations. It is not sufficient to assume independent electrons interacting with an average potential, but one has to consider the interaction between each pair of electrons explicitly. In the spectra, this leads to excitons and multiplets that dominate the spectral line-shape.
In this talk I will discuss these various forms of core level spectroscopy, which material properties one can obtain with these techniques and how to theoretically understand these spectra. During the tutorial, I will introduce Quanty, (www.quanty.org) a versatile many body quantum script language that allows one to relatively easily write small programs that can calculate core level spectra of a variety of materials using different levels of approximation or models.

## Slide 2
Core level spectroscopy
of transition metal and rare earth compounds
http://www.thphys.uni-heidelberg.de/~haverkort/talks/
Maurits W. Haverkort
Institute for theoretical physics, Heidelberg University, Heidelberg, Germany
M.W.Haverkort@thphys.uni-heidelberg.de

## Slide 3
Challenges in solid state physics / chemistry
Important for technology
Important in biochemistry (active centers of enzymes)
Often open shell systems, involved to understand

## Slide 4
Transition metal compounds; a large variety of properties
Metal insulator transitions
M. Marezio et al.,
PRB 5, 2541 (1972)
P. B. Allen et al.,
PRB 48, 4359 (1993)
VO2
Resistivity (Wcm)

## Slide 5
Transition metal compounds; a large variety of properties
High-Tc superconductivity

## Slide 6
Transition metal compounds; a large variety of properties
Active centers in enzymes
Fe in Heme
Mn role in photosynthesis

## Slide 7
Spin
Orbital
Lattice
Charge
Interaction between the charge, lattice, orbital and spin

## Slide 8
Spin arrangements (element resolved of TM multilayers)
Valence and local symmetry of TM compounds
Orbital occupation (the d-shell is 5 fold degenerate)
dyz
dxz
dxy
dx2-y2
d3z2-r2
Need tools to measure
And excitations (spin-waves – magnons – orbital excitations)
Spectroscopy
(x-ray spectroscopy)
How the low energy Hamiltonian emerges from the full Hamiltonian

## Slide 9
Spectroscopy as a tool to test and learn
PES
Optics

## Slide 10
X-ray spectroscopy as a tool to test and learn
PES
XAS
RXD
RIXS
nIXS

## Slide 11
Second talk
RXD
RIXS
nIXS

## Slide 12
First talk
PES
XAS
Slide 92
Slide 14

## Slide 13
Start with X-ray Absorption Spectroscopy
2p

## Slide 14
X-ray Absorption Spectroscopy – some observations
Data L. H. Tjeng et al.

## Slide 15
X-ray Absorption Spectroscopy – some observations
2p
Data L. H. Tjeng et al.

## Slide 16
X-ray Absorption Spectroscopy – some observations
Valence dependence – ground state symmetry determines the line shape
Data L. H. Tjeng et al.

## Slide 17
X-ray Absorption Spectroscopy – some observations
2p
Polarized XAS
Sensitive to
Orbital occupation
Natural linear dichroism
C. T. Chen et al PRL 68, 2543 (1992)

## Slide 18
X-ray absorption spectroscopy – Spin sensitive
2p
700
720
740
760
Photon energy (eV)
Polarized XAS
Sensitive to
Magnetic moments
Magnetic circular dichroism
J. Stöhr, J. Elec. Spec. Rel. Phonom. 75, 253 (1995).

## Slide 19
X-ray Absorption Spectroscopy – some observations
Polarized XAS
Sensitive to
Magnetic moments
Magnetic linear dichroism
2p
P. Kuiper et al., PRL 70, 1549 (1993)

## Slide 20
X-ray absorption spectroscopy – a band picture
1s

## Slide 21
Final state
Initial state
Dipole (transition) operator
Energy conservation
X-ray absorption spectroscopy – one electron selection rules
Fermi’s golden rule

## Slide 22
X-ray absorption spectroscopy – one electron selection rules

## Slide 23
X-ray absorption spectroscopy – one electron selection rules

## Slide 24
X-ray absorption spectroscopy – one electron selection rules

## Slide 25
X-ray absorption spectroscopy – one electron selection rules
C. T. Chen et al. Phys. Rev. Lett. 68, 2543 (1992)

## Slide 26
X-ray absorption spectroscopy – correlations in the d-shell
2p

## Slide 27
Use NiO as an example material
Ni2+ - 4s0 3d8
O2- - 2p6

## Slide 28
Partly filled degenerate d-shell – in LDA NiO is a metal

## Slide 29
X-ray absorption spectroscopy – correlations in the d-shell
2p
Experiment is sharper than LDA empty density of states
Branching ratio (L2, L3 intensity ratio is not 3:2)
Experiment shows more structure (multiplets) than DOS

## Slide 30
X-ray absorption spectroscopy – correlations in the d-shell
2p
Experiment is sharper than LDA empty density of states
Branching ratio (L2, L3 intensity ratio is not 3:2)
Experiment shows more structure (multiplets) than DOS

## Slide 31
In LDA NiO is a metal: Experimentally it is a good insulator
F. J. Morin, Phys. Rev. 93, 1199 (1954)
R. Newman and R. M. Chrenko,
Phys. Rev 114 1507 (1959)
Room temperature
r~105 O cm
Optical-gap
3.5 – 4.0 eV
Conductivity (W-1 cm-1)
Temperature-1

## Slide 32
Mott-Hubbard insulator
Energy gain W
Energy cost U
Difference between anti-ferromagnetic Neel order and spin-singlet configurations
vs.

## Slide 33
Mott-Hubbard insulator
Keep all correlations on a single central site – use a (dynamical) mean-field approximation for the rest of the solid.

## Slide 34
correlations in the d-shell
2p

## Slide 35
correlations in the d-shell
2p

## Slide 36
correlations in the d-shell
2p

## Slide 37
correlations in the d-shell
2p

## Slide 38
correlations in the d-shell
2p

## Slide 39
correlations in the d-shell
2p

## Slide 40
correlations in the d-shell
2p

## Slide 41
correlations in the d-shell
2p

## Slide 42
correlations in the d-shell
2p

## Slide 43
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
Core – valence interaction
W=1
U=20
Q=0

## Slide 44
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=0.25

## Slide 45
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=0.5

## Slide 46
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.0

## Slide 47
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.25

## Slide 48
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.5

## Slide 49
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.75

## Slide 50
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=2.0
Exciton
Continuum edge jump

## Slide 51
X-ray absorption spectroscopy – excitons
2p

## Slide 52
X-ray absorption spectroscopy – excitons
2p

## Slide 53
Local many body calculations based on parameters

## Slide 54
Ligand field theory for NiO
Ni2+ - 4s0 3d8
O2- - 2p6

## Slide 55
Orbital energy level diagram
t2g
eg

## Slide 56
Coulomb repulsion
dxy
dx2-y2
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 57
Coulomb repulsion
dxy
dx2-y2
dz2
Coulomb repulsion is smaller when electrons are farther apart

## Slide 58
Coulomb repulsion
dx2-y2
dz2
dxy
dxy
Coulomb repulsion is smaller when electrons are farther apart

## Slide 59
XAS final state for NiO 2p53d9
Ni – 2p
Ni – 3d
L3 edge
L2 edge

## Slide 60
Local many body calculations based on parameters
Parameters
Size of the Coulomb interaction
Size of the crystal-field

## Slide 61
Can we calculate these parameters?
Parameters
Size of the Coulomb interaction
Size of the crystal-field
Notes: -

## Slide 62
Obtain parameters from LDA

## Slide 63
In LDA NiO is a metal: Experimentally it is a good insulator
F. J. Morin, Phys. Rev. 93, 1199 (1954)
R. Newman and R. M. Chrenko,
Phys. Rev 114 1507 (1959)
Room temperature
r~105 O cm
Optical-gap
3.5 – 4.0 eV
Conductivity (W-1 cm-1)
Temperature-1

## Slide 64
Although NiO is a metal in LDA, there are many things correct

## Slide 65
“Downfold” the DFT results to obtain basis of choice

## Slide 66
Pick a basis of “TM-d” and “O-p” Wannier orbitals

## Slide 67
Full multiplet ligand field model based on DFT

## Slide 68
How to calculate 2p X-ray Absorption Spectroscopy
2p
Start from LDA potential
Create Wannier functions
On this basis and potential build local Hamiltonian including all local many body interactions
Solve by exact diagonalization
Phys. Rev. B 85, 165113 (2012)
Theory
Experiment

## Slide 69
Two levels of theory, how to decide which one to use
nIXS
Example of d-d excitations in NiO

## Slide 70
Correlations, Multiplets and entanglement
An example from d-d excitations NiO
M. W. Haverkort et al. PRB 85, 165113 (2012)

## Slide 71
NiO some basic properties
t2g
eg

## Slide 72
First peak, excitation from t2g to eg
M. W. Haverkort et al. PRB 85, 165113 (2012)
First peak, understandable on the level of LDA+U

## Slide 73
Third peak – Coulomb repulsion
dxy
dx2-y2
dz2
Coulomb repulsion is smaller when electrons are farther apart

## Slide 74
Third peak – Coulomb repulsion
dx2-y2
dz2
dxy
dxy
Coulomb repulsion is smaller when electrons are farther apart

## Slide 75
Third peak – Coulomb repulsion
M. W. Haverkort et al. PRB 85, 165113 (2012)
Third peak understandable on the level of time dependent LDA+U

## Slide 76
Second peak, double excitation from t2g to eg
M. W. Haverkort et al. PRB 85, 165113 (2012)
Need to go beyond mean field theory

## Slide 77
Second peak, double excitation from t2g to eg
M. W. Haverkort et al. PRB 85, 165113 (2012)
Warning!!! A single photon can only excite a single electron. The reason you see these strong double excitations is a true quantum many-body effect!
- Need to solve locally the full many-body problem

## Slide 78
Two levels of theory, how to decide which one to use
Correlations give rise to additional peaks in the spectrum

## Slide 79
Example on an H2 molecule
1s
1s

## Slide 80
Time dependent perturbation theory
Fermi’s golden rule
Green’s function – spectral representation (energy domain)
Green’s function – (time domain)

## Slide 81
Time dependent perturbation theory
Green’s function – (time domain)
At time t=0 an excitation is created
In spectroscopy one probes if at time t the excitation is still at the same place, or if it moved away.
Spectroscopy probes the dynamics of the system

## Slide 82
Example on an H2 molecule
1s
1s

## Slide 83
Example on an H2 molecule
1s
1s

## Slide 84
Example on an H2 molecule
1s
1s

## Slide 85
Example on an H2 molecule
Excitation energy
Intensity

## Slide 86
Example on an H2 molecule – with correlations

## Slide 87
Example on an H2 molecule – with correlations

## Slide 88
Example on an H2 molecule – with correlations

## Slide 89
Example on an H2 molecule – with correlations

## Slide 90
Example on an H2 molecule – with correlations
Excitation energy
Intensity

## Slide 91
Example on an H2 molecule – with correlations
Excitation energy
Intensity
1s
1s

## Slide 92
Core level photo electron spectroscopy
PES

## Slide 93
Example on Gold (Au)
PES

## Slide 94
Example on Gold (Au)

## Slide 95
Example on Gold (Au)
Au – [Xe] 6s2 5d9

## Slide 96
Example on Gold (Au)
Au – [Xe] 5d10 6(sp)1

## Slide 97
Example on Gold (Au) – 5d and 6s

## Slide 98
Example on Gold (Au) – 5p

## Slide 99
Example on Gold (Au) – 5s

## Slide 100
Example on Gold (Au) – 4f

## Slide 101
Example on Gold (Au) – 4d

## Slide 102
Example on Gold (Au) – 4p

## Slide 103
Example on Gold (Au) – 4s
760 eV or
880000 Kelvin

## Slide 104
Naming conventions
n | l | j | degeneracy | edge
1 | s | 1/2 | 2 | K
2 | s | 1/2 | 2 | L1
 | p | 1/2 | 2 | L2
 |  | 3/2 | 4 | L3
3 | s | 1/2 |  | M1
 | p | 1/2 |  | M2
 |  | 3/2 |  | M3
 | d | 3/2 |  | M4
 |  | 5/2 |  | M5
4 | s | 1/2 |  | N1
 | p | 1/2 |  | N2
 |  | 3/2 |  | N3
 | … |  |  | 
N1
N2
N3
N4
N5
N6,7

## Slide 105
Example on Gold (Au) – valence band

## Slide 106
Example on Gold (Au) – valence band

## Slide 107
Example on Gold (Au) – valence band
Experiment

## Slide 108
Example on Gold (Au) – valence band
Experiment
Density functional theory
s
p
d

## Slide 109
Example on Gold (Au) – valence band
Experiment
Density functional theory
s
p
d

## Slide 110
Example on Gold (Au) – valence band

## Slide 111
Example on Gold (Au) – valence band

## Slide 112
Example on Gold (Au) – 4f core level

## Slide 113
Example on Gold (Au) – XPS

## Slide 114
2p3/2 PES of Ni metal is not a delta function

## Slide 115
2p3/2 PES of Ni metal is not a delta function

## Slide 116
2p3/2 PES of Ni metal is not a delta function

## Slide 117
PES
Edge singularity – a model with core-valence interaction
Core – valence interaction: Q

## Slide 118
PES
Edge singularity – a model with core-valence interaction

## Slide 119
PES
Edge singularity – a model with core-valence interaction

## Slide 120
PES
Edge singularity – a model with core-valence interaction

## Slide 121
PES
Edge singularity – a model with core-valence interaction

## Slide 122
PES
Edge singularity – a model with core-valence interaction

## Slide 123
PES
Edge singularity – a model with core-valence interaction

## Slide 124
PES
Edge singularity

## Slide 125
PES
Edge singularity – a model with core-valence interaction

## Slide 126
PES
Edge singularity – a model with core-valence interaction

## Slide 127
PES
Edge singularity – a model with core-valence interaction

## Slide 128
PES
2p3/2 PES of Ni metal is not a delta function

## Slide 129
4f7/2 PES of Au metal is not a delta function

## Slide 130
4f7/2 PES of Au metal is not a delta function

## Slide 131
4f7/2 PES of Au metal is not a delta function

## Slide 132
PES
2p3/2 PES of Ni metal is not a delta function
Core – valence interaction: Q

## Slide 133
Multiple peaks from metal to correlated metal to insulator
PES
Groundstate: y = a s0 + b s1 + g s2
Final states: Energy:
cs0 ½ U + Q
cs1 0
cs2 ½ U - Q
cs1
cs2
cs0

## Slide 134
Multiple peaks from metal to correlated metal to insulator
PES
Multiple peaks can be used to determine mixed valence contributions to ground-state – measure of correlations
For an fully itinerant system the different possible valences are statistically distributed.
example of H2 molecule
For a strongly correlated system only one valence contributes to the ground-state.
example of H2 molecule
Groundstate: y = a s0 + b s1 + g s2
y = ½ s0 + ¼ s1 + ½ s2
Groundstate: y = a s0 + b s1 + g s2
y = 0 s0 + 1 s1 + 0 s2

## Slide 135
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 136
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 137
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 138
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 139
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 140
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 141
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 142
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 143
correlations in the d-shell
DMFT
Locally all correlations
Non-local mean-field
See talk of Silke?

## Slide 144
Multiple peaks from metal to correlated metal to insulator
PES
cs1
cs2
cs0

## Slide 145
Multiple peaks from metal to correlated metal to insulator
PES
cs1
cs2
cs0

## Slide 146
Multiple peaks from metal to correlated metal to insulator
PES
cs1
cs2
cs0

## Slide 147
Multiple peaks from metal to correlated metal to insulator
PES
cs1
cs2
cs0

## Slide 148
Multiple peaks from metal to correlated metal to insulator
PES
cs1
cs2
cs0

## Slide 149
2p PES of CuO is truly not a delta function
PES

## Slide 150
Electronic structure of CuO
Cu2+ - 4s0 3d9
O2- - 2p6

## Slide 151
2p PES final state for CuO 2p53d9 and 2p53d10L
Groundstate locally: y = a d9 + b d10L
Energy
d9 0
d10L D
Final states Energy
cd9 0
cd10L D-Q

## Slide 152
CuO
PES

## Slide 153
2p PES final state for CuO 2p53d9
Ni – 2p
Ni – 3d
L3 edge
L2 edge

## Slide 154
A) At some point in time the photon gets absorbed, the photon disappears and the electron in the s-shell is excited to the p-shell
Quiz: what happens when a photon hits an atom?
For example an H atom with one electron in the s-shell
B) Photons are electromagnetic waves. The electron starts to oscillate around the nucleus with the photon frequency
C) Electrons are particles. The photon bounces like a ball of the electron, thereby transferring part of its energy to the electron
Notes: I know that the 1s to 2p excitation of H is not in the x-ray range ( ¾ Rydberg, 10.2 eV) but all our theories are conveniently rather independent from the actual energy scale. (Linear response does not depend on the value of omega) For the purist replace H by Fe25+ (also a single electron around a nucleus, but as Z=26 in this case the excitation energy is 26^2 * ¾ = 507 Rydberg or 6898 eV)