## Slide 1: Core level spectroscopy of transition metal and rare earth compounds
Transition metal and rare earth compounds show a wealth of different properties. They are used as materials for energy storage (battery compounds), dyes in solar cells, elements in the read head of hard disks, high temperature superconductors, or the active centers in many of the known enzymes. The large variety of tunable properties of these materials is related to the large number of low energy degrees of freedom of the transition metal or rare earth ion. Correlations between the electrons in a solid lead to a detailed interplay between the local spin, charge, orbital and lattice degrees of freedom. The result is extremely rich physics of these open shell systems. At the same time the interplay between several low energy degrees of freedom make these materials involved to understand. Although enormous theoretical progress has been made during the last years in the understanding of correlated materials one often needs experimental input to understand particular phenomenon.
Core level spectroscopy in many cases turns out to be a very efficient method to study the many body properties of these systems. Core level photoelectron spectroscopy allows one to determine how the low energy Hamiltonian arises from the high-energy scale interactions. It thus provides information on the low energy model parameters of the system. X-ray absorption spectroscopy contains information on the local electronic structure. It provides information on the symmetry of the wave function, such as the local spin-state or orbital occupation. Resonant x-ray diffraction is related to x-ray absorption, in addition to x-ray absorption it allows one to study the special dependence of local electronic order in the system. Resonant inelastic x-ray scattering allows one to study the dynamics of low energy excitations. Non-resonant inelastic x-ray scattering of core level excitations is a technique rather comparable to x-ray absorption spectroscopy with the difference that it allows for non-dipole transitions, useful in the study of involved orbital or multipole ordering.
For the understanding of these spectra, in this class of materials, it is important to realize that one needs to treat the interactions between the electrons beyond mean field approximations. It is not sufficient to assume independent electrons interacting with an average potential, but one has to consider the interaction between each pair of electrons explicitly. In the spectra, this leads to excitons and multiplets that dominate the spectral line-shape.
In this talk I will discuss these various forms of core level spectroscopy, which material properties one can obtain with these techniques and how to theoretically understand these spectra. During the tutorial, I will introduce Quanty, (www.quanty.org) a versatile many body quantum script language that allows one to relatively easily write small programs that can calculate core level spectra of a variety of materials using different levels of approximation or models.

## Slide 2
Core level spectroscopy
of transition metal and rare earth compounds
http://www.thphys.uni-heidelberg.de/~haverkort/teaching/
Maurits W. Haverkort
Institute for theoretical physics, Heidelberg University, Heidelberg, Germany
M.W.Haverkort@thphys.uni-heidelberg.de

## Slide 3
A) At some point in time the photon gets absorbed, the photon disappears and the electron in the s-shell is excited to the p-shell
Quiz: what happens when a photon hits an atom?
For example an H atom with one electron in the s-shell
B) Photons are electromagnetic waves. The electron starts to oscillate around the nucleus with the photon frequency
C) Electrons are particles. The photon bounces like a ball of the electron, thereby transferring part of its energy to the electron
Notes: I know that the 1s to 2p excitation of H is not in the x-ray range ( ¾ Rydberg, 10.2 eV) but all our theories are conveniently rather independent from the actual energy scale. (Linear response does not depend on the value of omega) For the purist replace H by Fe25+ (also a single electron around a nucleus, but as Z=26 in this case the excitation energy is 26^2 * ¾ = 507 Rydberg or 6898 eV)

## Slide 4
Interaction of photons with matter
RIXS
nIXS

## Slide 5
Interaction of photons with matter
RIXS
nIXS

## Slide 6
Final state
Initial state
Energy conservation
Response theory (linear)
Fermi’s golden rule

## Slide 7
Response theory (linear)
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 8
Response theory (linear)
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 9
Response theory (linear)
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 10
First order response functions
Response theory
Higher order response functions (two photon, second order)

## Slide 11
Second talk
RXD
RIXS
nIXS
XAS
Slide 63
Slide 17
Slide 98
Slide 115

## Slide 12
Need tools to measure: Orbital, Spin, Charge
2p
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Technique developed in late 1980’s
Fink, Sawatzky, Fuggle
Thole, van der Laan
Chen, Sette

## Slide 13
Resonant X-ray Diffraction (RXD)
2p
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Hannon, Trammel, Bloom, Gibbs
Phys. Rev. Lett. 61, 1245 (1988)
Phys. Rev. B 43, 5663 (1991)
Cara, Thole
Rev. Mod. Phys. 66, 1509 (1994)

## Slide 14
Resonant X-ray Diffraction (RXD)
Resonant Inelastic X-ray Scattering (RIXS)
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Theory prediction of magnetic excitations
J. Luo, G. T. Trammell, and J. P. Hannon,
Phys. Rev. Lett. 71, 287 (1993).
F.M.F. de Groot, P. Kuiper, and G. A. Sawatzky,
Phys. Rev. B 57, 14584 (1998).
Experimental realization
L. Braicovich, G. Ghiringhelli, N. B. Brookes, et al.
Phys. Rev. Lett. 102, 167401 (2009).
2p

## Slide 15
non-resonant Inelastic X-ray Scattering (IXS)
3p
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Resonant X-ray Diffraction (RXD)
Resonant Inelastic X-ray Scattering (RIXS)
Nobelprize Compton
Light elements – band excitations:
Keijo Hämäläinen, W. Schulke
Excitonic excitations TM and RE compounds:
B. C. Larson et al. PRL 99, 026401 (2007)
M. W. Haverkort et al. PRL 99, 257401 (2007)
R. A. Gordon, et al. EPL 81, 26004 (2008)
T. Willers, et al. PRL 109, 046401 (2012)

## Slide 16
3p
non-resonant Inelastic X-ray Scattering (IXS)
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge

## Slide 17
Compton scattering
The Nobel Prize in Physics 1927
Data R. Gordon et al.
CeO2

## Slide 18
Compton scattering
The Nobel Prize in Physics 1927
Data R. Gordon et al.
CeO2

## Slide 19
Compton scattering
The Nobel Prize in Physics 1927
Data R. Gordon et al.
CeO2

## Slide 20
Compton scattering
The Nobel Prize in Physics 1927
Data R. Gordon et al.
CeO2
Resonances
(4d to 4f excitation)

## Slide 21
Compton scattering
The Nobel Prize in Physics 1927
Data R. Gordon et al.
CeO2
Resonances
(4d to 4f excitation)

## Slide 22
Compton scattering
The Nobel Prize in Physics 1927
Data R. Gordon et al.
CeO2
Resonances
(4d to 4f excitation)
These are resonances
in non-resonant IXS

## Slide 23
Bulk-sensitive XAS characterization of light elements
U. Bergmann, P. Glatzel, S. P. Cramer
Microchemical Journal 71, 221 (2002)
IXS
XAS
Resonances
(1s to 2p excitation)
C

## Slide 24
Not so light elements – clear dd excitations in NiO and CoO
B. C. Larson et al.
Phys. Rev. Lett. 99, 026401 (2007).

## Slide 25
Two years later with good statistics and fine structure
Experiment:
R. Verbeni, et al. J. Synchrotron Rad. 16, 469 (2009).
Ab initio theory:
M. W. Haverkort et al. PRB 85, 165113 (2012).

## Slide 26
And even clear core-valence excitations in CeO2
R. A. Gordon, et al.
Euro. Phys. Lett. 81, 26004 (2008)

## Slide 27
And even clear core-valence excitations in CeO2
R. A. Gordon, et al.
Euro. Phys. Lett. 81, 26004 (2008)

## Slide 28
And even clear core-valence excitations in CeO2
R. A. Gordon, et al.
Euro. Phys. Lett. 81, 26004 (2008)

## Slide 29
And in U and Th compounds
J. A. Bradley et al.
Phys. Rev. B 81, 193104
(2010).
Subhra Sen Gupta et al.
Phys. Rev. B 84, 075134
(2011).

## Slide 30
How can one understand these spectra?
Good intensities (spectra in less than an hour) in some cases
Strong momentum dependence, independent of the Brillouine zone
In CeO2 at the 4d to 4f edge, the energy of the d to f excitations shift by 20 eV depending if one looks in forward scattering or backward scattering…

## Slide 31
Non-resonant inelastic x-ray scattering

## Slide 32
Non-resonant inelastic x-ray scattering

## Slide 33
Non-resonant inelastic x-ray scattering

## Slide 34
Non-resonant inelastic x-ray scattering

## Slide 35
Non-resonant inelastic x-ray scattering
Dynamical (charge) structure factor

## Slide 36
Introducing atomic form factors for excitonic excitations
Dispersion within a Brillouine zone
Bloch waves
“Atomic” form factor
For example localized Wannier orbitals

## Slide 37
Atomic like orbitals as basis states in a solids

## Slide 38
Atomic like orbitals as basis states in a solids

## Slide 39
Atomic like orbitals – Multipole expansion

## Slide 40
Multipole expansion – |q| dependence

## Slide 41
Multipole expansion – |q| dependence
Experiment: B. C. Larson et al. PRL 99, 026401 (2007) – Theory: M. W. Haverkort et al. PRL 99, 257401 (2007).

## Slide 42
Multipole expansion – |q| dependence
J. A. Bradley et al.,
Phys. Rev. B 84, 205105 (2011).
R. A. Gordon, et al.
Euro. Phys. Lett. 81, 26004 (2008)
Phys. Rev. Lett. 99, 257401 (2007)
Why are the multipole excitations at lower energy so much sharper and thus clearer to see?

## Slide 43
Multipole expansion – |q| dependence
R. A. Gordon, et al.
J. Phys.: Conf. Series 190, 012047
(2009)

## Slide 44
Multipole expansion – |q| dependence
J. A. Bradley et al.
Phys. Rev. B 81, 193104
(2010).
Subhra Sen Gupta et al.
Phys. Rev. B 84, 075134
(2011).

## Slide 45
Multipole expansion – |q| dependence
5d to 5f in Actanides
4d to 4f in Lanthanides
3p to 3d in Transition metal compounds

## Slide 46
Multipole expansion – |q| dependence
5d to 5f in Actanides
4d to 4f in Lanthanides
3p to 3d in Transition metal compounds
Core – valence coulomb interaction

## Slide 47
Multipole expansion – |q| dependence
5d to 5f in Actanides
4d to 4f in Lanthanides
3p to 3d in Transition metal compounds
Multiplet splitting

## Slide 48
Multipole expansion – |q| dependence
5d to 5f in Actanides
4d to 4f in Lanthanides
3p to 3d in Transition metal compounds
Interaction with continuum

## Slide 49
Multipole expansion – |q| dependence
J. A. Bradley et al.
Phys. Rev. B 81, 193104
(2010).
Subhra Sen Gupta et al.
Phys. Rev. B 84, 075134
(2011).

## Slide 50
Multipole expansion – direction of q dependence
N. Hiraoka et al.,
Euro. Phys. Lett. 96, 37007 (2011).

## Slide 51
Multipole expansion – direction of q dependence
Experiment:
R. Verbeni, et al. J. Synchrotron Rad. 16, 469 (2009).
Ab initio theory:
M. W. Haverkort et al. PRB 85, 165113 (2012).

## Slide 52
Multipole expansion – direction of q dependence

## Slide 53
Multipole expansion – direction of q dependence
Single transition

## Slide 54
Multipole expansion – direction of q dependence
Double transition

## Slide 55
Multipole expansion – direction of q dependence

## Slide 56
Multipole expansion – direction of q dependence

## Slide 57
Multipole expansion – direction of q dependence
N. Hiraoka et al.,
Euro. Phys. Lett. 96, 37007 (2011).

## Slide 58
Angle dependence in cubic MnO

## Slide 59
Angle dependence in cubic MnO

## Slide 60
Ground-state wave-function in CeCu2Si2
Two possible ground-state symmetries in CeCu2Si2, that show exactly the same dipole spectra
Notes: ----- Meeting Notes (12/7/12 18:46) -----
explain collors
put atoms in there

## Slide 61
Solution – triacontadipole transitions
T. Willers et al.PRL 109, 046401 (2012)
Notes: ----- Meeting Notes (12/7/12 18:46) -----
explain collors
put atoms in there

## Slide 62
The use of higher than dipole transitions, as present in inelastic x-ray scattering allowed us to distinguish.
Important for ground-state symmetry of many 4f heavy fermion compounds
Could be important for the understanding of chemical binding in 5f compounds:
(Am, Pu, U, Th)
Notes: ----- Meeting Notes (12/7/12 18:46) -----
emphesise this entanglement
allowed us to dischtingus between the two orbitals

## Slide 63
Back to XAS
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
2p
Technique developed in late 1980’s
Fink, Sawatzky, Fuggle
Thole, van der Laan
Chen, Sette

## Slide 64
Two ways to calculate XAS

## Slide 65
Two ways to calculate XAS – bands
1s

## Slide 66
Two ways to calculate XAS – excitons
2p
Start from LDA potential
Create Wannier functions
On this basis and potential build local Hamiltonian including all local many body interactions
Solve by exact diagonalization
Phys. Rev. B 85, 165113 (2012)
Theory
Experiment

## Slide 67
Interpretation without theory – sum rules
2p
Theory
Experiment

## Slide 68
Sum rules for circular dichroism: orbital and spin momentum

## Slide 69
Sum rules for circular dichroism: orbital and spin momentum

## Slide 70
Sum rules for circular dichroism: orbital and spin momentum

## Slide 71
Sum rules for circular dichroism: orbital and spin momentum

## Slide 72
Sum rules for circular dichroism: orbital and spin momentum

## Slide 73
Sum rules for circular dichroism: orbital and spin momentum

## Slide 74
Sum rules for linear dichroism: orbital occupation

## Slide 75
XAS and the conductivity tensor (s) – an example for s to p
w0
Real
Imaginary
Absorption –Im[s]
(in Landau Lifschitz absorption is Re[s])

## Slide 76
But the conductivity tensor (s) is a TENSOR

## Slide 77
But the conductivity tensor (s) is a TENSOR
Absorption
–Im[e.s.e]

## Slide 78
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
x-polarized light

## Slide 79
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
y-polarized light

## Slide 80
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
z-polarized light

## Slide 81
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light

## Slide 82
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 83
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 84
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 85
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 86
The conductivity tensor (s) in cubic symmetry

## Slide 87
The conductivity tensor (s) in tetragonal symmetry

## Slide 88
The conductivity tensor (s) in orthorhombic symmetry

## Slide 89
The conductivity tensor (s) in monoclinic symmetry

## Slide 90
The conductivity tensor (s) in triclinic symmetry

## Slide 91
The conductivity tensor (s) in magnetic materials

## Slide 92
The conductivity tensor (s) in magnetic materials

## Slide 93
Sum rules for circular dichroism: orbital and spin momentum

## Slide 94
Thole et al.’s sum-rules in tensor form. s to p excitations

## Slide 95
Resonant X-ray Diffraction (RXD)
2p
And now momentum, i.e. spatial resolved, from XAS to RXD
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Hannon, Trammel, Bloom, Gibbs
Phys. Rev. Lett. 61, 1245 (1988)
Phys. Rev. B 43, 5663 (1991)
Cara, Thole
Rev. Mod. Phys. 66, 1509 (1994)

## Slide 96
An example magnetic Bragg reflection of Ho metal film
2p

## Slide 97
An example magnetic Bragg reflection of Ho metal film

## Slide 98
Absorption and diffraction – two sides of the same coin

## Slide 99
Crystalline sollid
Absorption and diffraction – two sides of the same coin
si
si
si
si
Each site gets polarized by the photon field and the local charge density starts to oscillate.
Absorption
Scattering

## Slide 100
2p
Relation between resonant x-ray diffraction and absorption
2p

## Slide 101
Diffraction at given momentum determined by the sum of local scattering with correct phase:
Crystalline sollid
Absorption and diffraction – two sides of the same coin
si
si
si
si
Each site gets polarized by the photon field and the local charge density starts to oscillate.
Absorption
Scattering

## Slide 102
An example magnetic Bragg reflection of Ho metal film

## Slide 103
Fundamental spectra from the literature

## Slide 104
Fundamental spectra from the literature

## Slide 105
Fundamental spectra from the literature

## Slide 106
Fundamental spectra from the literature

## Slide 107
An example magnetic Bragg reflection of Ho metal film

## Slide 108
Can we use sum-rules to get quantitative information

## Slide 109
Can we use sum-rules to get quantitative information

## Slide 110
Can we use sum-rules to get quantitative information

## Slide 111
Can we use sum-rules to get quantitative information

## Slide 112
Can we use sum-rules to get quantitative information

## Slide 113
Can we use sum-rules to get quantitative information

## Slide 114
Solve Maxwell's equations (with side conditions)

## Slide 115
2p
2p
And now excitations , from RXD to RIXS
2p
X-ray Absorption
Spectroscopy
Resonant X-ray
Diffraction
Resonant Inelastic
X-ray scattering

## Slide 116
Dispersing magnons

## Slide 117
Dispersing magnons – Neutron scattering
Interaction of Neutrons with matter is well understood (magnetic dipole),
single magnon intensity
q-dispersion
M. T. Hutchings and E. J. Samuelsen,
Phys. Rev. B 6, 3447 (1972)

## Slide 118
Recent development – measure spin dynamics with x-rays
Picture by G. Ghiringhelli and L. Braicovich
Resonant Inelastic
X-ray Scattering
RIXS
It now becomes feasible to measure the dynamics of low energy excitations in:
thin films
surfaces
Interfaces
nano-crystals
molecules

## Slide 119
RIXS – very high quality data on small samples
spinons
orbitons

## Slide 120
What is Resonant Inelastic X-ray Scattering (RIXS)
Outgoing light of
~ 0.5 to 10 keV
minus
10 meV to 10 eV
Incoming light of
~ 0.5 to 10 keV
Intermediate state with core hole and one extra valence electron

## Slide 121
Intermediate state
RIXS – what does one measure
Initial state
Final state

## Slide 122
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 123
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 124
RIXS – what is the cross section
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…

## Slide 125
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 126
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 127
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 128
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 129
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 130
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 131
XAS – XRD – RIXS – a time dependent picture

## Slide 132
XAS – XRD – RIXS – a time dependent picture in NiO
eg
t2g

## Slide 133
NiO – Ni 2p to Ni 3d excitation
eg
t2g
Ni-3d and O-2p on level of DMFT. (locally all interactions included)
Ni-3d and Ni-2p Coulomb interactions are local and included
After excitation Auger decay is possible, and included:
Ni-3d, Ni-3p, or Ni-3s scatters into the Ni-2p core hole and a Ni-3d, Ni-3p or Ni-3s orbital is emitted into es,p,d,f,g or h orbital

## Slide 134
NiO – Ni 2p to Ni 3d excitation
X-ray absorption of NiO (L23 edge) is well described.
How does the wave-function (charge density) evolve as a function of time when the sample is hit by an x-ray pulse?

## Slide 135
NiO – Ni 2p to Ni 3d excitation
eg
t2g
We include a light field of 1 kV per Angstrom (possible at SLAC) at an energy of 852 eV.
Pulse duration is 100 atto seconds
Upto c7 (4-th-order) response functions are included

## Slide 136
NiO 2p to 3d excitation in the time domain
1 kV Å-1
350 attosecond
holes in Ni 3d-shell
holes in Ni 2p-shell
FWHM 100 as
41 eV
Energy of pulse 852 eV

## Slide 137
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 138
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
BOOM
RIXS – what does one measure

## Slide 139
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 140
Challenge – No small parameter – perturbation theory fails
Different interactions are of similar scale
Perturbation theory leads to divergent series
i.e. summing part of the series gives a different result from the full solution!

## Slide 141
Intermediate state
Initial state
Final state
RIXS – what does one measure

## Slide 142
Understand RIXS by numerical solving a model
The equation to solve
with,
and

## Slide 143
Single Ni atom in crystal-field theory

## Slide 144
Hubbard model on finite (12) size cluster

## Slide 145
Understand RIXS as effective operator
Replace the exact RIXS operator by a low energy effective operator
Write the exact RIXS operator as a series
Possible operators in the series could be
Task: find all operators
and all coefficients

## Slide 146
Challenge – No small parameter – perturbation theory fails
Different interactions are of similar scale
Perturbation theory leads to divergent series
i.e. summing part of the series gives a different result from the full solution!

## Slide 147
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 148
Truncate at i=2
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 149
Truncate at i=4
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 150
Truncate at i=10
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 151
Truncate at i=20
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 152
Truncate at i=50
Divergent series – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as an expansion on powers of x:

## Slide 153
General problem in many particle physics

## Slide 154
General problem in many particle physics
Need for a non-divergent (non perturbative) series expansion

## Slide 155
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:

## Slide 156
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=1

## Slide 157
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=2

## Slide 158
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=3

## Slide 159
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=4

## Slide 160
Fourier v.s. Taylor – example from functions
The following function is smooth, continues and infinite differentiable on the real axis
We can write the function as a sum of orthonormal functions:
Truncate at n=5

## Slide 161
An alternative expansion for operators
Projection expansions for functions
Projection expansions for operators
with
if
with
if

## Slide 162
An alternative expansion for operators
Trivial example
with
and
an orthonormal complete set
we have
The trivial example needs exponentially many weird operators
Alternative:
Om,n an operator that transforms exponentially many states that share property n into states that share property m

## Slide 163
Expansion of the RIXS operator
Create a local (j) expansion
Lattice model

## Slide 164
Expansion of the RIXS operator
Lattice model
Site j
Create a local (j) expansion
Level L=0 only include operators acting on site j

## Slide 165
Expansion of the RIXS operator
Lattice model
Create a local (j) expansion
Level L=1 include operators acting on site j and n.n.
j

## Slide 166
Expansion of the RIXS operator
Lattice model
Create a local (j) expansion
Level L=2 include operators acting on site j, n.n. and n.n.n.
j

## Slide 167
Expansion of the RIXS operator
Lattice model
Create a local (j) expansion
Level L=3 include operators acting on site j, n.n., n.n.n. and n.n.n.n.
j
etc.

## Slide 168
Expansion of the RIXS operator
Convergence of this series is guaranteed by linear algebra!
define

## Slide 169
Expansion of the RIXS operator
Convergence of this series is guaranteed by linear algebra!
As RIXS intensity is bounded:
Sufficient condition to guarantee absolute convergence of series

## Slide 170
Example for doped Hubbard model
with
As a first step we need to create all possible Om,n
For L=0 we only look at local operators
The local Fock space is given by 4 states
Operators on that basis as
4 by 4 matrices

## Slide 171
For L=1 we look at two sites
Example for doped Hubbard model
Resulting in 162=256 operators
The Fock space is given by 16 states

## Slide 172
We can get back to more familiar representations by linear combing these operators (unitary transformation)
Example for doped Hubbard model
For L=0 (only keeping the particle number conserving operators)

## Slide 173
We can get back to more familiar representations by linear combing these operators (unitary transformation)
Example for doped Hubbard model
For L=1 (only keeping the particle number conserving operators)

## Slide 174
RIXS – effective operator – spin excitations
Effective operator for spin excitations only

## Slide 175
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
… and spin susceptibilities

## Slide 176
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
Theory
Experiment
s(0)=

## Slide 177
Predicted RIXS spectra with cross polarized light
spin susceptibility, same as neutron scattering

## Slide 178
General polarization: RIXS is a mixture of 1 and 2 spin flips

## Slide 179
Spin excitations in 1-dimension

## Slide 180
Spin excitations in 1 dimension – Sr2CuO3

## Slide 181
Dispersing orbitals
spinons
orbitons

## Slide 182
Dispersing orbitals

## Slide 183
Dispersing orbitals

## Slide 184
Additional literature
Core level spectroscopy of Solids
Frank M. F. de Groot and Akio Kotani
NEXAFS Spectroscopy
Joachim Stöhr
Introduction to ligand field theory (chapter 1 – 6)
Carl Johan Ballhausen (1962)
Physical Chemistry (chapter 13 – 18, (10 – 15) edition 5 (8))
Peter Atkins (2006)